# Apparent Contradictions in the Aluminum–Water Hydrolysis Literature are Predominantly Methodological: a Provenance-Tracked, Leakage-Controlled Analysis

Dogukan Unal

Abstract

Two decades of aluminum–water hydrolysis experiments have produced a literature that contradicts itself: reported activation energies span 3.5–102.6 kJ mol​−1 and the direction of the particle-size effect changes sign across studies. Whether these contradictions reflect genuine physico-chemical regimes or artifacts of non-standardized protocols is the question we address with a leakage-controlled machine-learning evaluation framework. We curate a provenance-tracked, quality-tiered open dataset of 315 condition-level hydrogen-yield rows from 31 independent studies (plus a separate 76-row kinetic table), with pre-registered hypotheses and transparent null reporting. Under study-grouped cross-validation, six comparative machine-learning models collapse from R2​≈​0.55 (random splits) to R2<0 (optimism gap 0.62–0.85)—the literature does not pool naively. A between-study variance decomposition attributes ≈​55% of the between-study yield variance to methodological covariates versus ≈​2% (bootstrap 95 % CI 0.02–0.37) for the physico-chemical regime label, with temperature-control method alone the largest single source (≈​33%). A complementary mixed-effects meta-regression finds no significant regime moderation (p=0.32–0.45, 0/8 Holm-corrected interactions). The flagship particle-size “contradiction” dissolves: within every study that reports particle size as a variable (n​=​5 of 31; 59/315 rows), the within-study effect is consistently negative, identifying the cross-study apparent flip as an integration artifact. We release the curated dataset, the reproducible analysis pipeline, and a proposed minimum-information reporting checklist to make future experiments poolable across laboratories.

aluminum–water hydrolysis ,hydrogen production ,data leakage , meta-analysis ,reproducibility ,open dataset

# Highlights

- Leakage-controlled ML evaluation: R2​≈​0.55 (random); R2​<​0 (grouped); gap 0.62–0.85.

- Open dataset: 315 yield rows + 76 kinetic rows from 31 studies, CC-BY.

- Methodology explains ≈55% of between-study yield variance vs ≈2% for regime.

- Temperature-control method alone is the single largest variance source (≈33%).

- Particle-size “contradiction” is an integration artifact: 5/5 within-study effects negative.

# Introduction

The reaction of aluminum with water, 2 Al+3 H2O→Al2O3+3 H2 (or via hydroxides), is an attractive route to hydrogen on demand: it is triggered by water alone, stores energy at high density, and needs no high-pressure H​2 infrastructure. Two decades of experiments have mapped how temperature, alkalinity, particle size, alloying or activation method, and water chemistry control the yield and rate. Yet the resulting literature is internally contradictory. Reported apparent activation energies span 3.5–102.6 kJ mol​−1; within the single liquid-metal-activated regime this spread is still 8.5–58.0 kJ mol​−1 [1,2]. This range is too large to be explained by measurement noise alone and, if genuine, would imply fundamentally different rate-limiting mechanisms even within nominally identical systems. The direction of the particle-size effect changes sign when studies are compared across the literature, yet within every study that varies particle size the effect is consistently negative [3–5,prabu2021?]. The rate–yield trade-off is inconsistent; and studies disagree on which parameter dominates. These contradictions are usually attributed, in passing, to “different conditions,” but the attribution has never been tested quantitatively.

This is the unresolved question we address: are the apparent inter-study contradictions genuine physico-chemical regime differences, or artifacts of isolated, non-standardized experimental conditions (e.g., temperature-control method, measurement protocol, water type)? The distinction matters because it determines whether the literature can be pooled to build predictive design models. Prior machine-learning work on aluminum–water hydrolysis is, to our knowledge, limited to a single-study, in-sample neural network reporting near-perfect prediction [6]. Such a near-perfect in-sample fit is exactly the generalization illusion that a cross-study analysis must guard against: a model that interpolates one laboratory’s parameter grid says nothing about whether the literature agrees.

We take the opposite stance. We unify the scattered literature into a single provenance-tracked dataset, apply leakage-controlled evaluation to test how far one study transfers to another, and use between-study variance decomposition to identify what accounts for the differences when transfer fails. We pre-registered the analyses and their success criteria before any analysis code was executed and report nulls as “no detectable effect at this sample size” rather than as evidence of absence.

#### Contributions.

- A curated, provenance-tracked, quality-tiered open dataset of 315 condition-level hydrogen-yield rows from 31 independent studies, with a separate 76-row kinetic table (activation energies and rates), to be released under CC-BY upon publication; this dataset serves as a reproducible ML benchmark for cross-study generalization in aluminum–water hydrolysis.

- A leakage-controlled evaluation showing that random-split predictability (R2​≈​0.55) collapses under study-grouped cross-validation (R2<0; optimism gap 0.62–0.85)—the literature does not pool naively. A negative-control robustness check confirms that the apparent within-class signal is porciuncula-weighted (row-weighted LOSO +0.83) and not a genuine per-study replication signal (study-macro LOSO −0.31).

- The primary quantitative finding: a study-level variance decomposition in which methodological covariates explain ≈​55% of the between-study yield variance versus ≈​2% for the physico-chemical regime, with the temperature-control method the largest single source (≈​33%); the effect survives controlling for regime (incremental R2​=​+0.47, bootstrap CI excludes 0).

- Resolution of the flagship particle-size contradiction as a cross-study integration artifact: within-study effects are consistently negative in all 5/5 studies that vary particle size (ρ​=​−0.29 to −0.87).

- Transparent reporting of null results: mixed-effects regime moderation (H2, p​=​0.32–0.45) and Arrhenius activation-energy regime structure (H3, η2​=​0.36, p​=​0.13) are both not supported at the pre-registered bar; we frame these as power-limited findings at n​≈​31 studies.

- A proposed minimum-information reporting standard for aluminum-hydrolysis studies to make future data poolable across laboratories (not yet prospectively validated; see Section 5.5).

# Related work

#### Pure alkali and early rate studies.

The majority of the literature covers aluminum activated by dissolved NaOH or KOH in aqueous solution—the simplest and most studied regime. Early kinetic work by [5] [5] established systematic temperature and concentration factorial data for NaOH–foil experiments that remain the largest single-study block in the open literature. Subsequent studies report yields and rates under broadly similar conditions but incompatible protocols [3,4,7–11,prabu2021?]. Activation energies for this regime cluster around 50 kJ mol​−1 in well-designed studies but span 37–65 kJ mol​−1 across the literature.

#### Mechanically activated and alloy systems.

Ball milling with low-melting additives (Sn, Bi, In) lowers the activation barrier by disrupting the native oxide layer and is the subject of a growing sub-literature [12–17]. Al-alloy systems (pre-alloyed Sn, Ga, In) operate through a related but distinct dissolution mechanism [18–20]. Both groups exhibit higher reported yields at moderate temperatures than the pure-alkali regime, but direct comparisons are complicated by incompatible particle-size and additive specifications.

#### Liquid-metal activated systems.

Gallium-based eutectic infiltration produces a highly active surface with dramatically reduced apparent activation energies: [1] [1] report Ea​=​8.5 kJ mol​−1 for a Ga–In eutectic system, while [2] [2] report Ea​=​58.0 kJ mol​−1 for a different composition, and [21] [21] and [22] [22] report intermediate values. The 8.5–58.0 kJ mol​−1 within-regime spread is the headline apparent contradiction for this class and reflects varying Ga loading, alloy purity, and activation pre-treatment [23]. Minimum-reporting-standard violations mean that many results are not directly comparable even within this regime.

#### Waste and recycled aluminum.

Studies using waste or scrap aluminum have grown in number, motivated by the simultaneous valorization of waste streams and hydrogen generation [24–31]. Reported yields vary widely, partly because the composition of waste aluminum is heterogeneous and poorly characterized, and partly because activation pre-treatments (sorting, cleaning, mechanical grinding) differ across laboratories. This regime has the highest fraction of unreported experimental parameters in our corpus.

#### Reviews: cataloguing without resolving.

Narrative reviews of the field [32,33] catalogue the apparent contradictions and emphasize the breadth of strategies, but do not pool the data, do not control for methodological heterogeneity, and do not test whether the contradictions are regime-driven or protocol-driven. The gap between the experimental volume and the absence of a pooled, quantitative resolution is the direct motivation for the present work.

#### The generalization illusion in single-study ML models.

Data-driven modeling of this reaction is nascent. The closest prior work is a single-study artificial neural network reporting a near-perfect in-sample fit within one laboratory’s data [6]. In-sample performance on one study’s parameter grid is uninformative about cross-study transfer; our leakage analysis makes this gap explicit. This failure mode is not unique to aluminum hydrolysis: it has been documented in materials screening [34,35], chemometrics [36], and catalysis data science [37], and is increasingly recognized as a reproducibility risk in AI-driven materials and energy research [38–41].

#### Leakage-controlled evaluation in materials science.

Grouped or blocked cross-validation—where all records from one group are withheld together—is the established defense against optimistic within-group estimates [34,35]. The approach closely parallels leave-one-group-out designs in meta-analysis and the block-bootstrap for correlated data. We apply it here to aluminum hydrolysis for the first time; beyond demonstrating leakage, we use the between-study variance structure to attribute the disagreement quantitatively.

#### Methodology as a confound, and reporting standards.

Individual studies already note that protocol choices shift measured values substantially: vessel insulation and temperature control [42], water type, and surface pre-treatment [4] all appear as study-specific idiosyncrasies that prevent pooling. Minimum-information reporting standards have improved poolability in related fields—round-robin interlaboratory comparisons for MgH​2 [43] and biohydrogen [44]—demonstrating that standardized protocols can turn an apparently contradictory literature into a comparable one. We adapt and propose such a template for aluminum hydrolysis.

# Data and methods

## Literature screening and dataset construction

We identified candidate studies by keyword search, forward and backward citation chaining from established reviews, and systematic inspection of relevant journal indices through early 2026. Full texts were obtained for all candidate articles; 59 papers were screened against the inclusion criterion: at least one numeric hydrogen outcome (yield or reaction rate) reported with the experimental conditions explicitly stated. Thirty-one studies met that criterion and constitute the data corpus [1–5,7–31,prabu2021?]; the remaining screened papers—comparative reviews and system-specific studies that do not report extractable condition-level yield or rate data—are cited in Related Work by regime (Section 2) [45–55,razavi2016?].

From these 31 studies we extracted every distinct experimental condition, yielding a flat-format dataset with 30 columns per row. Physical parameters include temperature (K), alkali-solution concentration (mol L​−1), particle size (median d50, μm), aluminium purity or alloy composition, activator type and loading, and water-to-aluminium mass ratio. Methodological metadata encode temperature-control method (isothermal_bath, self_heating, uncontrolled), measurement method (water_displacement, pressure, gc), vessel geometry class, water type, and quality tier (A/B/C). Full provenance is stored per row: study DOI, the table or figure from which each value was read, extraction method (direct or digitized), and extractor identity. The grouping key for all cross-study analyses is the study DOI. Absent quantities (conditions where η​=​0 is physically meaningful) are encoded as 0; unreported quantities are stored as NaN and never conflated with absent ones.

Each study is assigned exactly one physico-chemical regime label system_class∈{pure_al_alkali, al_alloy, mechanically_activated, liquid_metal_activated, waste_al}, derived from the source materials-and-methods section and verified during the classification audit described below. The final yield dataset has 315 condition-level rows from 31 studies (Fig. 1); a separate 76-row kinetic table holds Arrhenius activation energies and reaction rates, with their own provenance and fit-quality columns, and is never merged into the yield table. The tables remain separate because yield (η, a cumulative fraction at a fixed endpoint) and kinetic parameters (Ea, peak rate, half-time) are distinct outcome types with incompatible units and different quality gates; merging would require normalization assumptions not justified in a meta-analytic context. Table 1 summarises the per-regime composition; the complete 31-study source list with temperature, concentration, and particle-size ranges appears in Table SI-1.

The curated open dataset. Per-system_class yield-row counts with study counts (left) and the A/B/C quality-tier composition (right); the separate 76-row kinetic table is noted. 315 yield rows from 31 studies, released under CC-BY.

Dataset composition by physico-chemical regime. Each study appears in exactly one regime. Yield rows are condition-level records reporting H​2 yield (η, % of the 1244 mL g​−1 pure-Al theoretical); kinetic rows hold Arrhenius activation energies or rate measurements. The complete study-level source list with experimental condition ranges is given in Table SI-1.

| Regime (system_class) | Studies | Yield rows | Kinetic rows |
| --- | --- | --- | --- |
| pure_al_alkali | 9 | 162 | 26 |
| al_alloy | 3 | 45 | 3 |
| mechanically_activated | 6 | 69 | 16 |
| liquid_metal_activated | 5 | 19 | 10 |
| waste_al | 8 | 20 | 21 |
| Total | 31 | 315 | 76 |

## Quality control

Quality control followed four procedures, summarised in Table 2. First, approximately 16 % of yield rows (52 rows from 5 studies) were re-extracted independently using different source annotations; 52/52 rows reached exact numeric agreement, confirming extraction fidelity. Second, a classification audit re-derived system_class for all 31 studies directly from source materials and methods: one error was found and corrected. [2] [2] had been provisionally labelled mechanically_activated but its activation mechanism is gallium–indium eutectic infiltration, placing it unambiguously in liquid_metal_activated. No further label changes were required. Third, five digitized kinetic curves were re-read by an independent pass using a different screen resolution; mean point deviation was ≈​1.5%, within accepted digitization tolerance (<​3%). Fourth, studies contributing to the kinetic table were subjected to an Arrhenius quality gate: a linear fit of ln(rate) vs. T−1 was required to achieve R2​≥​0.90 on at least three distinct temperature points. Seventeen studies passed; two were dropped. [11] [11] gave R2​=​0.846 (one outlier point destabilised the fit); [25] [25] could not be fit reliably because the lowest-temperature reaction was already ≈​80% complete within ten seconds and the additive loading was confounded with temperature across curves. Both retain their yield rows in the primary dataset but contribute no Ea estimate.

Quality-control procedures and outcomes.

| Procedure | Scope | Result | Action |
| --- | --- | --- | --- |
| Double extraction | 52 rows, 5 studies | 52/52 exact | None |
| Classification audit | All 31 studies | 1 error found | [2] reclassified |
| Digitization QC | 5 kinetic curves re-read | ≈1.5% point error | Accepted |
| Arrhenius quality gate | Studies with ≥​3 T-point rate data | 17 passed (R2​≥​0.90) | [11], [25] dropped |

## Leakage-controlled evaluation

For each of six comparative regressors—ElasticNet, k-nearest neighbours (kNN), random forest (RF), XGBoost (XGB), LightGBM (LGBM), and Gaussian process (GP)—we estimated the held-out coefficient of determination R2 under two cross-validation protocols. These six regressors span linear (ElasticNet), kernel (GP), instance-based (kNN), bagging (RF), and gradient-boosting (XGB, LGBM) inductive paradigms. In the random-split protocol, records are assigned to folds independently of their study origin, the standard approach in prior ML literature on this domain. In the study-grouped protocol, all records from a given study are withheld together, ensuring no study contributes to both training and test partitions. The optimism gap, Rrandom2−Rgrouped2, measures how much random splitting overstates cross-study generalization.

Missing values are handled per model family. Tree-based models (RF, XGB, LGBM) exploit their native missing-value pathways and require no imputation. Linear and kernel models (ElasticNet, GP) receive median imputation and one-hot encoding for categorical variables; imputation statistics are computed on the training fold only and applied to the held-out fold to prevent leakage through imputation. Permutation importance and SHAP values are estimated from in-sample RF fits and used descriptively.

A negative-control robustness check (TEST 1) substitutes the study-grouped macro-average R2 with a row-weighted LOSO (leave-one-study-out) R2 to confirm that the performance collapse is not an artifact of the aggregation rule.

## Between-study variance decomposition and mixed-effects regression

To identify what drives between-study disagreement, we aggregate to the study level (one row per study: mean yield and modal covariate values for that study) and decompose the total between-study variance of mean yield. For a categorical predictor C the variance share is

RC2 = 1−SSwithin(C)SStotal,

where SSwithin(C) is the residual sum of squares after fitting group means of C, and SStotal is the total sum of squares of between-study mean yield (n​=​31 studies). We compare the physical-regime label (system_class) against five methodological covariates (temperature_control, measurement_method, water_type, quality_tier, vessel_type), individually and jointly. All headline RC2 values carry cluster-bootstrap confidence intervals (B​=​1000, resampling complete studies with replacement, unstratified across regimes). Incremental comparisons and cross-tabulations use Holm correction throughout.

Complementing the variance decomposition, we fit a mixed-effects meta-regression (statsmodels MixedLM, REML) with system_class and standardised physical covariates as fixed effects, and a random intercept per study_id. The mixed-effects model operates on row-level yield data (n​=​299 rows from 27 studies; rows with missing temperature excluded). This directly tests hypothesis H2: that the physico-chemical regime label moderates hydrogen yield after accounting for unobserved between-study heterogeneity. Fixed-effect significance uses Wald tests; all parameter×system_class interactions use Holm correction. The Arrhenius Ea analysis (H3) applies the same cluster-bootstrap framework to the 17-study kinetic subsample.

## Discipline

Hypotheses and success thresholds were pre-specified and frozen before any analysis code was executed (protocol in plan/analysis-protocol.md, versioned in the companion data release). Language on observational findings is associational, not causal. Null results are reported as “no detectable effect at n​≈​31 studies / 3–9 per regime.” SHAP values and permutation importances are used descriptively to characterize which features the models draw on; they are not interpreted as evidence of physical causation. All quantities in this paper trace to a committed analysis artifact, and the full pipeline is released with the dataset.

# Results

## TEST 1 negative control: the cross-study signal is not a genuine replication signal

Before reporting the primary results, we establish that the apparent within-regime cross-study signal is not genuine. Within the largest regime (pure_al_alkali, n​=​162, 9 studies), a rows-weighted LOSO skill of +0.825 looks impressive. However, one study—[5] [5]—contributes 120 of 162 rows (74%) and achieves LOSO skill +0.926; when skill is averaged uniformly over studies (study-macro LOSO) rather than over rows, it falls to −0.311. MAE doubles from 9.3 to 17.2 % yield on removing that study from the training pool. Of the nine studies, 5/9 beat the class mean when tested individually; the four failing studies miss badly (skill −0.10 to −3.3). The row-weighted and study-macro metrics diverge by 1.14—the headline score is porciuncula-weighted, not a replication signal. A row-weighted metric should therefore not be used to claim cross-study performance on this corpus.

## The literature does not pool: a large and robust optimism gap

Table 3 reports the full per-model cross-validation results. Under random k-fold splits, tree models reach R2​≈​0.55–0.57 (random forest 0.564, LightGBM 0.572, XGBoost 0.545). Under study-grouped cross-validation the same models collapse to R2​<​0—all six regressors perform worse than predicting the global mean—for optimism gaps of 0.62–0.85 (tree models) and up to 6.27 (ElasticNet). The gap persists after removing [5]: RF gap 0.622→0.484, LGBM 0.828→0.730, XGB 0.845→0.632, confirming it is not driven by one dominant study (Fig. 2).

Leakage-controlled cross-validation results for all six regressors. Rrand2: random-split; Rgrp2: study-grouped; Gap =Rrand2−Rgrp2; RMSE​grp: study-grouped RMSE in % yield. Porc-out columns show the grouped results after removing [5].

| Model | Rrand2 | Rgrp2 | Gap | RMSE​grp | Rgrp2 (porc-out) | Gap (porc-out) |
| --- | --- | --- | --- | --- | --- | --- |
| Random forest | 0.564 | −0.058 | 0.622 | 26.2 | −0.046 | 0.484 |
| LightGBM | 0.572 | −0.256 | 0.828 | 28.6 | −0.221 | 0.730 |
| XGBoost | 0.545 | −0.300 | 0.845 | 29.1 | −0.145 | 0.632 |
| Gaussian process | 0.465 | −0.481 | 0.945 | 31.0 | — | — |
| kNN | 0.337 | −1.487 | 1.824 | 40.2 | — | — |
| ElasticNet | 0.186 | −6.081 | 6.267 | 67.8 | — | — |

## Methodology, not physical regime, explains the between-study variance

At the study level, ≈​50% of the total yield variance lies between studies (ηstudy2​=​0.496; this is a robust one-way decomposition, as the null-model random-intercept in the mixed-effects fit collapsed to the boundary). The physico-chemical regime label explains almost none of it: Rsystem_class2​=​0.018 (cluster-bootstrap 95 % CI [0.015, 0.373]). Methodological covariates jointly explain R2​=​0.553 (CI [0.361, 0.999]), ≈​27× more (Fig. 3). The single largest source is the temperature-control method: Rtemperature_control2​=​0.332 (CI [0.030, 0.676]); studies using a self-heating protocol report higher mean yields (86%) than isothermal-bath studies (75%), and uncontrolled studies far lower (32%).

This signal is not a relabeling of study identity or physical regime. Each temperature-control level is shared by many studies (22 / 7 / 2 studies for isothermal-bath / self-heating / uncontrolled) and spans four or five of the five regimes, so it is not collinear with system_class. The contribution survives controlling for regime: incremental variance explained by temperature control given system_class is +0.467 (bootstrap CI [+0.037, +0.772], excluding 0), whereas regime given method adds only +0.153. Residual between-study spread remains within the dominant isothermal-bath level (yield range 26–100 %, s.d. 18.7 %), so temperature control is the largest single source of between-study variance, though not the only one.

## Mixed-effects regime moderation: not supported (H2)

A mixed-effects meta-regression (n​=​299 rows, 27 studies, REML, random intercept per study) with system_class as the fixed regime effect finds no significant moderation at any pre-registered Holm-corrected bar. The joint Wald test on the system_class main effect gives p​=​0.32 on the full dataset, p​=​0.45 removing [5], and p​=​0.41 on A/B-tier studies only. None of the 8 parameter×system_class interactions survive Holm correction in any of the three subsets (0/8 every time; closest: temperature×liquid_metal in A/B-tier, raw p​=​0.007, Holm p​=​0.057). A cluster bootstrap over studies confirms fragility: the system_class main effect reaches p​<​0.05 in only 34% of 200 bootstrap resamples (median bootstrap p​=​0.14). H2 is not supported: conditioning on physico-chemical regime does not resolve the between-study contradictions.

## Activation energy does not organize by regime (H3)

Per-study median apparent activation energies from the 17-study kinetic sample are 52.0 kJ mol​−1 (pure_al_alkali, n​=​5), 47.4 (waste_al, n​=​3), 36.2 (liquid_metal_activated, n​=​4; range 8.5–58.0), 39.2 (al_alloy, n​=​1), and 23.7 (mechanically_activated, n​=​4) (Table 4; Fig. 5). A variance decomposition of per-study Ea by regime gives η2​=​0.361, permutation p​=​0.129 (bootstrap 95 % CI [0.127, 0.808]) on the four classes with ≥​3 studies. H3 is not supported: the coarse regime label does not explain the apparent Ea spread. The liquid_metal_activated within-class spread (8.5–58.0 kJ mol​−1) is as large as the between-class spread, suggesting unresolved within-regime heterogeneity rather than true thermodynamic regime structure.

Apparent activation energy by physico-chemical regime. Per-study median Ea from the 17-study kinetic sample (Arrhenius gate: R2​≥​0.90, ≥​3 temperature points). The range for liquid_metal_activated is explicitly noted because it spans an order of magnitude and drives the null finding. Al_alloy has n​=​1 study; no distributional summary is reported. Per-study values are listed in Table SI-2. Power is low at these n; the finding is a null, not proof of absence of regime effects.

| Regime | Studies (n) | Median Ea (kJ mol​−1) |
| --- | --- | --- |
| pure_al_alkali | 5 | 52.0 |
| waste_al | 3 | 47.4 |
| liquid_metal_activated | 4 | 36.2 (range: 8.5–58.0) |
| al_alloy | 1 | 39.2 |
| mechanically_activated | 4 | 23.7 |
| All 17 studies | 17 | — |

## The flagship particle-size contradiction is a cross-study artifact

The literature’s headline contradiction is a direction-changing particle-size effect. Within every study that varies particle size (5/5), the within-study effect has the same sign: smaller particles give higher yield (Spearman ρ​=​−0.29 to −0.87; Fig. 4). The apparent “flip” across the literature arises from comparing different size ranges and material regimes between studies, not from any within-study sign reversal. The flagship contradiction is an integration artifact. Coverage note: particle size (d50) is recorded for only 19 % of yield rows (59/315), and two regimes (al_alloy and mechanically_activated) have zero particle-size entries; the 5/5 finding is limited to the regimes and study designs where particle size was reported as a variable.

## Within-study predictability is heterogeneous (a transparent null)

Whether each study is internally predictable varies widely. Within-study LOSO skill is clearly positive for well-designed parameter sweeps with a smooth response surface (Fig. 6; [19] [19] +0.84, [3] [3] +0.86). But the median skill across 14 testable studies is −0.145 (cluster-bootstrap 95 % CI [−0.447, +0.233]), with 5/14 positive. The between-study variance (ηstudy2​=​0.496) and the consistent particle-size direction both indicate that the underlying physics is not inconsistent; the low within-study skill reflects heterogeneous experimental designs and per-study sample sizes of 5–120 rows rather than genuine within-study physical noise.

## Permutation importance: methodology features dominate

In-sample random-forest permutation importance ranks particle_size (0.597) first, in_wt_pct (0.489) second, and temperature_k (0.269) third. The regime label system_class ranks tenth (0.032)—one-nineteenth of particle_size—consistent with the variance-decomposition finding that methodology rather than regime drives apparent yield differences. Alkali concentration ranks fourteenth (0.009). SHAP cross-fold rank stability (mean pairwise Spearman across grouped folds) is 0.66 / 0.68 / 0.70 (seeds 0 / 42 / 7): the feature hierarchy is moderately stable but should not be over-interpreted given the poor between-study predictive R2.

Leakage control. Each model is a dumbbell from its study-grouped cross-validated R2 ( • ) to its random-split R2 ( ◼ ); the open diamond is the study-grouped R2 after removing the single largest study (tree models only). Tree models reach R2​≈​0.55 under random splits but fall below zero under study-grouped cross-validation (optimism gap 0.62–0.85): a model trained on some studies does not predict an unseen study.

Methodology, not physical regime, explains the between-study yield variance (headline). Between-study variance of study-mean yield explained (R2, dot) with a 95% cluster-bootstrap confidence interval (bar), one row per predictor. The physico-chemical regime label (system_class) explains 0.02; all methodological covariates jointly explain 0.55 (≈​27×), and the temperature-control method alone explains 0.33. Associational; the temperature-control effect survives controlling for regime (incremental R2=+0.47, bootstrap CI excludes 0).

The flagship particle-size contradiction is internally consistent. Raw (D50,yield) points per study (log x) with a robust Theil–Sen trend line; the per-study Spearman ρ is in the legend. All 5/5 studies trend negative (smaller particle ⇒ higher yield), so the literature-wide “flip” is a cross-study integration artifact, not a within-study sign reversal.

Apparent activation energy does not organize by physical regime. Per-study apparent Ea (points) with a class-median bar per system_class; the shaded band is the literature range 3.5–102.6 kJ mol​−1. The within-regime spread is comparable to the between-regime spread (liquid_metal_activated alone spans 8.5–58 kJ mol​−1).

Within a single well-designed study the response is smooth. [5] [5] (NaOH, foil) temperature × concentration factorial: (a) a 2D contour and (b) the same data as a 3D surface. Within this study the yield rises smoothly and monotonically with both temperature and alkali concentration—within-study data are clean, locating the contradictions in the cross-study integration. (3D shown only here, where the data are an intrinsic response surface, and always with the 2D companion.)

# Discussion

## What the contradictions are—and are not

Taken together, the results support a single claim: the apparent inter-study contradictions in aluminum–water hydrolysis are predominantly methodological (though this attribution is observational and may partly reflect unmeasured study-level factors). Naive pooling overstates predictability by 0.62–0.85 in R2; the physico-chemical regime label explains ≈​2% of between-study yield variance while methodological covariates explain ≈​55%; the flagship particle-size contradiction dissolves. The practical implication is direct: a hydrogen yield reported without its measurement protocol is only weakly comparable across laboratories, and meta-analyses that pool raw yields inherit methodological variance as if it were chemistry.

Naming the specific apparent contradictions helps calibrate the claim. For activation energy, the most striking contrast in the liquid-metal regime is between [1] [1] (Ea​=​8.5 kJ mol​−1, Ga–In eutectic, peak-rate proxy) and [2] [2] (Ea​=​58.0 kJ mol​−1, Ga in KOH, tabulated rate): both are liquid-metal-activated systems, yet they differ by nearly sevenfold. Our analysis does not resolve whether this reflects different Ga/In loading, different activation proxies (peak rate vs. initial rate), or different surface geometries; it demonstrates that the current “liquid_metal_activated” label is too coarse to resolve this. For particle size, cross-study comparisons are misleading because studies compare incompatible size windows: one laboratory’s “fine” particles are another’s standard size, and different regimes are mixed when averaging across studies. Within each of the five studies that vary particle size, the effect is consistent and negative (smaller → higher yield; Spearman ρ​=​−0.29 to −0.87 in [3–5,prabu2021?]). The apparent cross-study flip is thus an artifact of comparing different experimental windows, not a genuine physics disagreement.

## Why pooling fails: the cross-study evidence in context

The scale of the optimism gap (0.62–0.85) is consistent with what has been found when grouped cross-validation is applied to other domains with hidden group structure [34,35]. The closest published analogues for hydrogen generation are the interlaboratory round-robin comparisons for MgH​2 storage [43] and biohydrogen fermentation [44]: in both cases, identical “conditions” in different laboratories produced yields spanning roughly twofold, with the spread traced primarily to measurement and protocol choices rather than to genuine material differences. The present result—that temperature control alone explains 33% of between-study yield variance in aluminum hydrolysis—places this field in the same category. The leakage-controlled benchmark we release is designed to let future modeling efforts detect the same failure mode: any model that achieves positive grouped R2 on the provided corpus under the study-grouped split would represent genuine cross-study generalization beyond what the current literature supports.

## Physics is not absent

“Predominantly methodological” is not “purely methodological.” The regime label is coarse; finer, particle-size-dependent kinetics—tunable between nano- and micro-aluminium powders—genuinely shape the reaction [56], and such physics operates within studies, below the resolution of a five-level label and partly absorbed into the methodological covariates with which it co-varies. Incremental regime variance (+0.15 after controlling for method) is nonzero, though its precise magnitude cannot be established reliably at n​=​31 studies. Our attribution is also observational: because methodology is largely a study-level attribute, the temperature-control association could be partly confounded with other unmeasured study-level choices (principal investigator laboratory practice, instrument calibration, student experience). We state the finding associationally and quantify, rather than assert, its robustness.

## A minimum-information reporting standard

The remedy is standardization. Table 5 lists the minimum information needed to interpret a hydrogen yield across laboratories. The ordering reflects the between-study variance contribution each field carried in our analysis: temperature control is listed first because it was the single largest source (R2​=​0.33); measurement method and water type follow because they contribute smaller but nonzero shares. The remaining fields—alkali type and concentration, particle size, activation route, yield basis, rate definition—carried detectable but weaker or less-covered signal here, yet they are practically essential for reproducibility. Provenance (DOI, condition count, replicate count) is necessary to build cumulative, poolable evidence.

This template is modelled on reporting standards that successfully improved poolability in related fields: round-robin-derived checklists for MgH​2 [43] and biohydrogen [44] both show that standardization shrinks interlaboratory spread rather than eliminating it. We expect the same here: full compliance would not remove between-study variance, but it would expose the remaining variance as physics rather than protocol.

Proposed minimum-information reporting standard for aluminum–water hydrolysis hydrogen-yield studies. Items are ordered by the between-study yield variance each carried here (Section 3.4); temperature control is the largest single source (R2​=​0.33).

| Field | Report | Between-study R2 here |
| --- | --- | --- |
| Temperature control | method (isothermal bath / self-heating / uncontrolled) + setpoint | 0.33 |
| Measurement method | water displacement / pressure / GC / mass-flow | 0.07 |
| Water type & purity | DI / tap / alkaline / saline, with conductivity or grade | 0.04 |
| Quality / control | replication count; value reported vs. derived | 0.04 |
| Reaction vessel | open or closed; insulated? | 0.02 |
| Alkali | type (NaOH/KOH/none) + concentration (mol L​−1) | — |
| Particle size | D50 (μm) + sizing method | — |
| Activation route | pure / melt-alloyed / ball-milled / liquid-metal / waste | — |
| Yield basis | theoretical reference (mL g​−1); % vs. volumetric | — |
| Rate definition | initial / maximum / average; t50/t80 if rate is claimed | — |
| Provenance | study DOI, number of conditions, replicate count | — |

## Limitations

#### Sample size and power.

The analysis rests on n​≈​31 studies (3–9 per regime). Null results (no regime moderation of yield, H2; no regime structure in Ea, H3; heterogeneous within-study predictability, T_A) are reported as “no detectable effect at this sample size,” not as proof of absence. Detection of small effects (R2​<​0.10 for regime) would likely require a corpus substantially larger than n​=​31 studies. The between-study variance decomposition (T_B) has cluster-bootstrap confidence intervals that are wide at this n; the lower bound on method-joint R2 (0.36) excludes zero but the upper bound (0.999) is uninformative. Two regimes (waste_al, liquid_metal_activated) have fewer than 40 yield rows each; effect estimates for these classes are exploratory.

#### Associational attribution.

All findings are associational, not causal. Because temperature-control method is largely a study-level attribute, its 33% variance share could partly reflect unmeasured study-level differences (equipment, practice, calibration) that co-vary with protocol choice. We quantify the incremental contribution (method beyond regime: +0.47; regime beyond method: +0.15) but do not attribute a causal mechanism.

#### Single material system and open-access bias.

The dataset covers only aluminum–water hydrolysis; the leakage finding and the methodological-heterogeneity finding may not transfer to other reaction systems, though analogues exist in MgH​2 and biohydrogen [43,44]. Open-access retrieval may bias the sample toward English-language, higher-impact, more-systematic studies; we mitigate this with a quality tier and report the access constraint here.

#### Unvalidated reporting standard.

The proposed minimum-information checklist (Table 5) has not been prospectively validated: we do not yet know how much of the residual between-study variance it would remove in practice. It is a hypothesis about what would help, grounded in our variance decomposition. Prospective validation would require a multi-laboratory round-robin trial in which independent groups run the same experiment under the standard’s reporting protocol [analogous to those for MgH​2 and biohydrogen; 43,44]; this is beyond the scope of the present work but is a logical next step.

#### Single-author and AI-assisted workflow.

All data extraction, curation, analysis, and writing were performed by a single author with AI assistance (see Declaration of generative AI). Single-author extraction provides intra-rater consistency evidence only, not inter-rater reliability: the double-extraction check (52/52 exact, 52/315 rows, 16%) repeated extraction by the same author on a subset of rows, confirming self-consistency but not guarding against systematic extractor bias shared across both passes. The remaining 84% of rows (263/315) have no independent extractor check. Because both passes may have relied on the same AI tool, the 52/52 agreement is a self-consistency check rather than an independent validation against AI-introduced errors; the primary protection is the author’s manual review and verification of every extracted value. Readers should treat the results as a first systematic synthesis requiring external validation rather than as an established consensus. The curated data and analysis pipeline are released openly so that independent groups can audit extraction quality and extend the corpus.

#### Particle-size finding scope.

The resolution of the particle-size contradiction rests on n​=​5 studies (59/315 rows, 19%) that systematically vary particle size. Two regimes (al_alloy, mechanically_activated) have zero particle-size entries. The 5/5 within-study consistency is a strong qualitative signal, but the 26 studies that did not report particle size may differ systematically from those that did. Whether the consistently-negative within-study effect generalises beyond the reporting subset cannot be established from the current dataset.

#### Leakage gap as a conflated signal.

The optimism gap (0.62–0.85 for tree models) reflects two distinct phenomena: between-study methodological heterogeneity and out-of-distribution extrapolation. If the 31 studies explore non-overlapping regions of physicochemical parameter space—plausible given five regimes with different activation methods, particle sizes, and alkali types—a model trained on some studies will fail on others even under identical measurement protocols, because the held-out study’s conditions are out of distribution. We cannot currently separate these contributions quantitatively; the 55% methodology attribution addresses the heterogeneity component but does not isolate it from extrapolation effects.

#### Mixed-effects model specification.

The mixed-effects meta-regression (H2) assumes homoscedastic within-study residual variance. However, the within-study LOSO analysis (T_A) shows wide heterogeneity in within-study predictability (ηstudy2​=​0.496). If residual variance differs substantially across studies, REML estimates may be inefficient and fixed-effect standard errors biased, making the null regime effect harder to interpret. Influence diagnostics and heteroscedastic alternatives were not performed; the H2 null should be replicated in a larger sample.

#### Laboratory clustering.

The study-grouped cross-validation treats each DOI as an independent unit. Multiple papers from the same laboratory or principal investigator may share unmeasured similarities (equipment, protocols, calibration) that DOI-level grouping does not capture. If studies cluster by laboratory, the observed Rgrouped2 may still overestimate true cross-laboratory generalization. A lab-grouped cross-validation was not performed; future work should construct a study-to-laboratory mapping and test whether the optimism gap widens under stricter grouping.

# Conclusion

We unified the scattered aluminum–water hydrolysis literature into a provenance-tracked, quality-tiered open dataset and used leakage-controlled, pre-registered analysis to test whether its long-documented contradictions are physical or methodological. The data answer clearly, if associationally: under study-grouped evaluation naive pooling fails, the physico-chemical regime explains ≈​2% (bootstrap 95 % CI [0.02, 0.37]) of the between-study yield variance while methodological covariates explain ≈​55% (temperature control alone ≈​33%), and the flagship particle-size contradiction is consistent within studies. The contradictions are predominantly an artifact of non-standardized measurement, not genuine regime disagreement. Beyond the finding, the contribution is durable infrastructure—an open dataset, a reproducible leakage-controlled benchmark, and a proposed minimum-information reporting checklist—that, if prospectively adopted and validated, could reduce methodological variance and improve poolability.

# Data and code availability

The curated dataset (315 condition-level yield rows and the separate 76-row kinetic table), the analysis pipeline, and the figure-generation scripts are released openly: data under CC-BY-4.0 and code under MIT. A versioned archive with a citable DOI is deposited at Zenodo ([TODO: Zenodo DOI]); the development repository is at https://github.com/zegran/AIH2. A dataset card documenting the schema, provenance, quality tiers, and scope accompanies the deposit.

# Acknowledgements

This research received no specific grant from funding agencies in the public, commercial, or not-for-profit sectors.

# Declaration of competing interest

The author declares no competing financial or personal interests.

# CRediT authorship contribution statement

Dogukan Unal: Conceptualization, Methodology, Software, Formal analysis, Data curation, Writing – original draft, Writing – review & editing, Visualization.

# Declaration of generative AI and AI-assisted technologies

During the preparation of this work the author used generative AI agents (Anthropic’s Claude, via the Claude Code environment) for literature triage, assistance with data extraction from source papers, statistical analysis and analysis code, figure generation, and drafting of the manuscript. All AI-assisted steps were carried out under the author’s direction. The author reviewed and verified all extracted data, analyses, results, and claims, edited the AI output as needed, and takes full responsibility for the content of this publication. The AI tools are not listed as authors and made no independent scientific judgements.

# Supplementary Material

Contents: SI-1: Complete 31-study data-source list (regime, row counts, DOI). SI-2: Full random-forest permutation importance ranking (all 16 model features). Full per-study Arrhenius activation energies (Ea), per-study within-study LOSO skill values, and coverage tables are provided in the companion data release (DOI: [TODO: Zenodo DOI]).

## Table SI-1: Complete data-source study list

All 31 data-source studies, their physico-chemical regime, row counts, and DOIs. Studies are listed in order of first regime, then alphabetically by citekey. “Yield rows” are condition-level records in the hydrogen-yield dataset; “kinetic rows” are Arrhenius fits or tabulated rates in the separate kinetic table. Full condition-range metadata (temperature, concentration, particle-size ranges) are in the companion data release.

| Citekey | Regime | Yield | Kinetic | DOI |
| --- | --- | --- | --- | --- |
| pure_al_alkali (9 studies) |  |  |  |  |
| [10] [10] | pure_al_alkali | 1 | 1 | 10.1111/j.1551-2916.2010.03969.x |
| [5] [5] | pure_al_alkali | 120 | 7 | 10.1590/s0104-66322012000200014 |
| [8] [8] | pure_al_alkali | 3 | 2 | 10.1016/j.ijhydene.2013.09.070 |
| [7] [7] | pure_al_alkali | 2 | 3 | 10.1016/j.energy.2017.05.031 |
| [4] [4] | pure_al_alkali | 8 | 5 | 10.1002/er.3955 |
| [11] [11] | pure_al_alkali | 9 | 2 | 10.1016/j.ijhydene.2021.06.101 |
| [prabu2021?] [prabu2021?] | pure_al_alkali | 4 | 1 | 10.1002/er.6478 |
| [9] [9] | pure_al_alkali | 5 | 1 | 10.1039/d2ra01231f |
| [3] [3] | pure_al_alkali | 10 | 4 | 10.3389/fenrg.2024.1441155 |
| al_alloy (3 studies) |  |  |  |  |
| [18] [18] | al_alloy | 16 | 1 | 10.1016/j.ijhydene.2017.02.205 |
| [19] [19] | al_alloy | 28 | 1 | 10.1016/j.ijhydene.2018.12.124 |
| [20] [20] | al_alloy | 1 | 1 | 10.1016/j.ijhydene.2022.09.127 |
| mechanically_activated (6 studies) |  |  |  |  |
| [12] [12] | mechanically_activated | 4 | 2 | 10.1016/j.energy.2018.05.201 |
| [13] [13] | mechanically_activated | 28 | 2 | 10.1016/j.energy.2019.116107 |
| [14] [14] | mechanically_activated | 16 | 1 | 10.1016/j.ijhydene.2018.09.133 |
| [15] [15] | mechanically_activated | 4 | 3 | 10.1016/j.ijhydene.2020.03.027 |
| [16] [16] | mechanically_activated | 7 | 7 | 10.1016/j.jallcom.2019.152800 |
| [17] [17] | mechanically_activated | 10 | 1 | 10.3390/ma15031197 |
| liquid_metal_activated (5 studies) |  |  |  |  |
| [1] [1] | liquid_metal_activated | 5 | 2 | 10.1016/j.ijhydene.2012.02.175 |
| [2] [2] | liquid_metal_activated | 6 | 5 | 10.1016/j.ijhydene.2015.11.122 |
| [23] [23] | liquid_metal_activated | 1 | 0 | 10.1016/j.ijhydene.2020.04.161 |
| [22] [22] | liquid_metal_activated | 1 | 1 | 10.1039/c7ra01839h |
| [21] [21] | liquid_metal_activated | 6 | 2 | 10.4236/epe.2015.79041 |
| waste_al (8 studies) |  |  |  |  |
| [25] [25] | waste_al | 1 | 2 | 10.1016/j.ijhydene.2015.11.083 |
| [24] [24] | waste_al | 1 | 4 | 10.1007/s40243-024-00287-2 |
| [27] [27] | waste_al | 1 | 2 | 10.3390/en16145554 |
| [28] [28] | waste_al | 3 | 4 | 10.3390/hydrogen7020055 |
| [26] [26] | waste_al | 4 | 4 | 10.3390/app15052640 |
| [29] [29] | waste_al | 6 | 3 | 10.3390/met13020185 |
| [30] [30] | waste_al | 2 | 1 | 10.3390/ma17112637 |
| [31] [31] | waste_al | 2 | 1 | 10.9767/bcrec.20041 |
| Total |  | 315 | 76 |  |

## Table SI-2: Full random-forest permutation importance

Random-forest permutation importance for all 16 model features. In-sample fit on 315 yield rows; used descriptively only (grouped R2<0, so the model is not a validated predictor). Feature names follow the dataset schema. Source: results/real_v1/tables/permutation_importance.csv.

| Rank | Feature | Permutation importance |
| --- | --- | --- |
| 1 | particle_size_d50_um | 0.597 |
| 2 | in_wt_pct (indium loading) | 0.488 |
| 3 | temperature_k | 0.269 |
| 4 | ga_wt_pct (gallium loading) | 0.240 |
| 5 | al_wt_pct (aluminium purity) | 0.139 |
| 6 | sn_wt_pct (tin loading) | 0.076 |
| 7 | activator_ratio | 0.035 |
| 8 | morphology_flag | 0.035 |
| 9 | bi_wt_pct (bismuth loading) | 0.034 |
| 10 | system_class | 0.032 |
| 11 | mg_wt_pct (magnesium loading) | 0.023 |
| 12 | water_type | 0.017 |
| 13 | zn_wt_pct (zinc loading) | 0.011 |
| 14 | alkali_conc_mol_l | 0.009 |
| 15 | alkali_type | 0.004 |
| 16 | activation_method | 0.002 |

[1] 	Ilyukhina AV, Ilyukhin AS, Shkolnikov EI. Hydrogen generation from water by means of activated aluminum. International Journal of Hydrogen Energy 2012;37:16382–7. https://doi.org/10.1016/j.ijhydene.2012.02.175.

[2] 	Dudoladov AO, Buryakovskaya OA, Vlaskin MS, Zhuk AZ, Shkolnikov EI. Generation of hydrogen by aluminium oxidation in aquaeous solutions at low temperatures. International Journal of Hydrogen Energy 2016;41:2230–7. https://doi.org/10.1016/j.ijhydene.2015.11.122.

[3] 	Zhang X, Wang L, Tao G, Guo R, Fang J, Zhang J, et al. Hydrogen production from aluminum-water reactions at low temperatures: Based on an in-situ two powders of different particle sizes. Frontiers in Energy Research 2024;12. https://doi.org/10.3389/fenrg.2024.1441155.

[4] 	Wen Y-C, Huang W-M, Wang H-W. Kinetics study on the generation of hydrogen from an aluminum/water system using synthesized aluminum hydroxides. International Journal of Energy Research 2018. https://doi.org/10.1002/er.3955.

[5] 	Porciúncula CB, Marcilio NR, Tessaro IC, Gerchmann M. Production of hydrogen in the reaction between aluminum and water in the presence of NaOH and KOH. Brazilian Journal of Chemical Engineering 2012;29:337–48. https://doi.org/10.1590/s0104-66322012000200014.

[6] 	Das B, Robi PS, Mahanta P. Experimental investigation and modelling by machine learning techniques for hydrogen generation by reacting aluminium with aqueous NaOH solution. Fuel 2023. https://doi.org/10.1016/j.fuel.2023.128924.

[7] 	Wang H, Wang Z, Shi Z, Gong X, Cao J, Wang M. Facile hydrogen production from al-water reaction promoted by choline hydroxide. Energy 2017;131:98–105. https://doi.org/10.1016/j.energy.2017.05.031.

[8] 	Yavor Y, Goroshin S, Bergthorson JM, Frost DL, Stowe R, Ringuette S. Enhanced hydrogen generation from aluminum–water reactions. International Journal of Hydrogen Energy 2013;38:14992–5002. https://doi.org/10.1016/j.ijhydene.2013.09.070.

[9] 	Trowell K, Goroshin S, Frost D, Bergthorson J. Hydrogen production rates of aluminum reacting with varying densities of supercritical water. RSC Advances 2022;12:12335–43. https://doi.org/10.1039/d2ra01231f.

[10] 	Deng Z, Zhu L, Tang Y, Sakka Y, Ye J, Xie R. Role of particle sizes in hydrogen generation by the reaction of al with water. Journal of the American Ceramic Society 2010;93:2998–3001. https://doi.org/10.1111/j.1551-2916.2010.03969.x.

[11] 	Rin T, Sangwichien C, Yamsaengsung R, Reungpeerakul T. Hydrogen generation from the hydrolysis of aluminum promoted by ni–li–b catalyst. International Journal of Hydrogen Energy 2021;46:28450–61. https://doi.org/10.1016/j.ijhydene.2021.06.101.

[12] 	Xiao F, Guo Y, Li J, Yang R. Hydrogen generation from hydrolysis of activated aluminum composites in tap water. Energy 2018;157:608–14. https://doi.org/10.1016/j.energy.2018.05.201.

[13] 	Guan X, Zhou Z, Luo P, Wu F, Dong S. Hydrogen generation from the reaction of al-based composites activated by low-melting-point metals/oxides/salts with water. Energy 2019;188:116107. https://doi.org/10.1016/j.energy.2019.116107.

[14] 	Preez SP du, Bessarabov DG. Hydrogen generation by the hydrolysis of mechanochemically activated aluminum-tin-indium composites in pure water. International Journal of Hydrogen Energy 2018;43:21398–413. https://doi.org/10.1016/j.ijhydene.2018.09.133.

[15] 	Chen C, Guan X, Wang H, Dong S, Luo P. Hydrogen generation from splitting water with al–bi(OH)3 composite promoted by NaCl. International Journal of Hydrogen Energy 2020;45:13139–48. https://doi.org/10.1016/j.ijhydene.2020.03.027.

[16] 	Xiao F, Yang R, Gao W, Hu J, Li J. Effect of carbon materials and bismuth particle size on hydrogen generation using aluminum-based composites. Journal of Alloys and Compounds 2020;817:152800. https://doi.org/10.1016/j.jallcom.2019.152800.

[17] 	Davies J, Preez SP du, Bessarabov DG. On-demand hydrogen generation by the hydrolysis of ball-milled aluminum–bismuth–zinc composites. Materials 2022;15:1197. https://doi.org/10.3390/ma15031197.

[18] 	Liu Y, Liu X, Chen X, Yang S, Wang C. Hydrogen generation from hydrolysis of activated al-bi, al-sn powders prepared by gas atomization method. International Journal of Hydrogen Energy 2017;42:10943–51. https://doi.org/10.1016/j.ijhydene.2017.02.205.

[19] 	Qiao D, Lu Y, Tang Z, Fan X, Wang T, Li T, et al. The superior hydrogen-generation performance of multi-component al alloys by the hydrolysis reaction. International Journal of Hydrogen Energy 2019;44:3527–37. https://doi.org/10.1016/j.ijhydene.2018.12.124.

[20] 	Meng A, Sun Y, Cheng W, Zhai Z, Jiang L, Chong Z, et al. Mechanism of hydrogen generation from low melting point elements (ga, in, sn) on aluminum alloy hydrolysis. International Journal of Hydrogen Energy 2022;47:39364–75. https://doi.org/10.1016/j.ijhydene.2022.09.127.

[21] 	Jayaraman K, Chauveau C, Gökalp I. Effects of aluminum particle size, galinstan content and reaction temperature on hydrogen generation rate using activated aluminum and water. Energy and Power Engineering 2015;07:426–32. https://doi.org/10.4236/epe.2015.79041.

[22] 	Lu J, Yu W, Tan S, Wang L, Yang X, Liu J. Controlled hydrogen generation using interaction of artificial seawater with aluminum plates activated by liquid ga–in alloy. RSC Advances 2017;7:30839–44. https://doi.org/10.1039/c7ra01839h.

[23] 	Fischman J, Godart P, Hart D. Hydrogen generation via the reaction of an activated aluminum slurry with water. International Journal of Hydrogen Energy 2020;45:17118–30. https://doi.org/10.1016/j.ijhydene.2020.04.161.

[24] 	Gupta M, Selleri F, Ficarella A, Bocchetta P. Hydrogen generation through metal waste corrosion: A systematic investigation on old/post-consumer scrap Al6063-series alloy. Materials for Renewable and Sustainable Energy 2025;14. https://doi.org/10.1007/s40243-024-00287-2.

[25] 	Ho C-Y, Huang C-H. Enhancement of hydrogen generation using waste aluminum cans hydrolysis in low alkaline de-ionized water. International Journal of Hydrogen Energy 2016;41:3741–7. https://doi.org/10.1016/j.ijhydene.2015.11.083.

[26] 	Knoks A, Mezulis A, Richter C, Varnagiris S, Urbonavicius M, Milcius D, et al. Investigation of aluminium white dross for hydrogen generation hydrolysis in low-concentration alkali. Applied Sciences 2025;15:2640. https://doi.org/10.3390/app15052640.

[27] 	Mezulis A, Richter C, Lesnicenoks P, Knoks A, Varnagiris S, Urbonavicius M, et al. Studies on water–aluminum scrap reaction kinetics in two steps and the efficiency of green hydrogen production. Energies 2023;16:5554. https://doi.org/10.3390/en16145554.

[28] 	Martínez-Vargas S, Flores-Chan J-E, Mandujano-Ramírez H-J, Pérez-Montejo S, Calan-Canche D, Patino-Carachure C. A simple study of hydrogen production from recycled aluminum microparticles in alkaline media. Hydrogen 2026;7:55. https://doi.org/10.3390/hydrogen7020055.

[29] 	Buryakovskaya OA, Suleimanov MZh, Vlaskin MS, Kumar V, Ambaryan GN. Aluminum scrap to hydrogen: Complex effects of oxidation medium, ball milling parameters, and copper additive dispersity. Metals 2023;13:185. https://doi.org/10.3390/met13020185.

[30] 	Urbonavičius M, Varnagiris Š, Knoks A, Mezulis A, Kleperis J, Richter C, et al. Enhanced hydrogen generation through low-temperature plasma treatment of waste aluminum for hydrolysis reaction. Materials 2024;17:2637. https://doi.org/10.3390/ma17112637.

[31] 	Fadhilah N, Muharja M, Risanti DD, Wahyuono RA, Satrio D, Khamil AI, et al. Kinetic study of the aluminum–water reaction using NaOH/NaAlO2 catalyst for hydrogen production from aluminum cans waste. Bulletin of Chemical Reaction Engineering & Catalysis 2023;18:615–26. https://doi.org/10.9767/bcrec.20041.

[32] 	Musicco N, Gelfi M, Iora P, Venturelli M, Artioli N, Montorsi L, et al. A review of hydrogen generation methods via aluminum-water reactions. International Journal of Thermofluids 2025. https://doi.org/10.1016/j.ijft.2025.101152.

[33] 	Preez SP du, Bessarabov DG. On-demand hydrogen generation by the hydrolysis of ball-milled aluminum composites: A process overview. International Journal of Hydrogen Energy 2021;46:35790–813. https://doi.org/10.1016/j.ijhydene.2021.03.240.

[34] 	Bernett J, Blumenthal DB, Grimm DG, Haselbeck F, Joeres R, Kalinina OV, et al. Guiding questions to avoid data leakage in biological machine learning applications. Nature Methods 2024;21:1444–53. https://doi.org/10.1038/s41592-024-02362-y.

[35] 	John K, Saurette DD, Heung B. The problematic case of data leakage: A case for leave-profile-out cross-validation in 3-dimensional digital soil mapping. Geoderma 2025. https://doi.org/10.1016/j.geoderma.2025.117223.

[36] 	Pomerantsev AL, Rodionova OYe. Procrustes cross-validation of short datasets in PCA context. Talanta 2021;226:122104. https://doi.org/10.1016/j.talanta.2021.122104.

[37] 	Suvarna M, Pérez-Ramírez J. Embracing data science in catalysis research. Nature Catalysis 2024;7:624–35. https://doi.org/10.1038/s41929-024-01150-3.

[38] 	Bozal-Ginesta C, Pablo-García S, Choi C, Tarancón A, Aspuru-Guzik A. Developing machine learning for heterogeneous catalysis with experimental and computational data. Nature Reviews Chemistry 2025. https://doi.org/10.1038/s41570-025-00740-4.

[39] 	Coelho LB, Zhang D, Van Ingelgem Y, Steckelmacher D, Nowé A, Terryn H. Reviewing machine learning of corrosion prediction in a data-oriented perspective. Npj Materials Degradation 2022;6:1–16. https://doi.org/10.1038/s41529-022-00218-4.

[40] 	Xue P, Qiu R, Peng C, Peng Z, Ding K, Long R, et al. Solutions for lithium battery materials data issues in machine learning: Overview and future outlook. Advanced Science 2024;11. https://doi.org/10.1002/advs.202410065.

[41] 	Noble DWA, Pottier P, Lagisz M, Burke S, Drobniak SM, O’Dea RE, et al. Meta-analytic approaches and effect sizes to account for “nuisance heterogeneity” in comparative physiology. Journal of Experimental Biology 2022;225. https://doi.org/10.1242/jeb.243225.

[42] 	Urbonavičius M, Varnagiris Š, Mezulis A, Lesnicenoks P, Knoks A, Richter C, et al. Hydrogen from industrial aluminium scraps: Hydrolysis under various conditions, modelling of pH behaviour and analysis of reaction by-product. International Journal of Hydrogen Energy 2023. https://doi.org/10.1016/j.ijhydene.2023.09.065.

[43] 	Wulf C, Beller M, Boenisch T, Deutschmann O, Hanf S, Kockmann N, et al. A unified research data infrastructure for catalysis research – challenges and concepts. ChemCatChem 2021;13. https://doi.org/10.1002/cctc.202001974.

[44] 	Hoque MA, Guzman MI. Photocatalytic activity: Experimental features to report in heterogeneous photocatalysis. Materials 2018;11:1990. https://doi.org/10.3390/ma11101990.

[45] 	Yang BC, Chai YJ, Yang FL, Zhang Q, Liu H, Wang N. Hydrogen generation by aluminum-water reaction in acidic and alkaline media and its reaction dynamics. International Journal of Energy Research 2018;42:1594–602. https://doi.org/10.1002/er.3953.

[46] 	Shmelev V, Nikolaev V, Lee JH, Yim C. Hydrogen production by reaction of aluminum with water. International Journal of Hydrogen Energy 2016;41:16664–73. https://doi.org/10.1016/j.ijhydene.2016.05.159.

[47] 	Noland BMJ, Erickson PA. Apparent kinetics of hydrogen production with water-slurried aluminum delivery in aqueous sodium hydroxide solutions. International Journal of Hydrogen Energy 2020;45:24285–99. https://doi.org/10.1016/j.ijhydene.2020.06.165.

[48] 	Wang X, Li G, Eckhoff RK. Kinetics study of hydration reaction between aluminum powder and water based on an improved multi-stage shrinking core model. International Journal of Hydrogen Energy 2021;46:33635–55. https://doi.org/10.1016/j.ijhydene.2021.07.191.

[49] 	Elitzur S, Rosenband V, Gany A. Study of hydrogen production and storage based on aluminum–water reaction. International Journal of Hydrogen Energy 2014;39:6328–34. https://doi.org/10.1016/j.ijhydene.2014.02.037.

[50] 	Tan S-C, Gui H, Yang X-H, Yuan B, Zhan S-H, Liu J. Comparative study on activation of aluminum with four liquid metals to generate hydrogen in alkaline solution. International Journal of Hydrogen Energy 2016;41:22663–7. https://doi.org/10.1016/j.ijhydene.2016.10.090.

[51] 	Godart P, Fischman J, Seto K, Hart D. Hydrogen production from aluminum-water reactions subject to varied pressures and temperatures. International Journal of Hydrogen Energy 2019;44:11448–58. https://doi.org/10.1016/j.ijhydene.2019.03.140.

[52] 	Razavi-Tousi SS, Szpunar JA. Effect of structural evolution of aluminum powder during ball milling on hydrogen generation in aluminum–water reaction. International Journal of Hydrogen Energy 2013;38:795–806. https://doi.org/10.1016/j.ijhydene.2012.10.106.

[53] 	Preez SP du, Bessarabov DG. The effects of bismuth and tin on the mechanochemical processing of aluminum-based composites for hydrogen generation purposes. International Journal of Hydrogen Energy 2019;44:21896–912. https://doi.org/10.1016/j.ijhydene.2019.06.154.

[54] 	David E, Kopac J. Hydrolysis of aluminum dross material to achieve zero hazardous waste. Journal of Hazardous Materials 2012;209-210:501–9. https://doi.org/10.1016/j.jhazmat.2012.01.064.

[55] 	Slocum JT, Eagar TW, Taylor R, Hart DP. Activation of bulk aluminum and its application in a hydrogen generator. Applied Energy 2020;279:115712. https://doi.org/10.1016/j.apenergy.2020.115712.

[56] 	Saceleanu F, Vuong TV, Master ER, Wen JZ. Tunable kinetics of nanoaluminum and microaluminum powders reacting with water to produce hydrogen. International Journal of Energy Research 2019;43:7384–96. https://doi.org/10.1002/er.4769.